## Slide 1
Polymer Pyrolysis
2014. 9. 23. SNU Presentation
Seungdo KIM, Professor/Director
Pyrolysis Research Laboratory
Hallym University

## Slide 2
Contents
1. Introduction of Pyrolysis
3. Pyrolysis Kinetics
4. Pyrolysis Reactor Design
2. Pyrolysis Mechanisms

## Slide 3
1. Introduction

## Slide 4: Introduction: Definition of pyrolysis
Pyrolysis = Pyro + Lysis
Thermal cracking of polymers
into smaller molecules
Polymerization
Reverse Reaction

## Slide 5: Introduction: Basic Principles
Attacking the weakest bond
  Related to bond dissociation energy
    C-C, C-H, C-O, C-Cl
More thermal energy input yields lower molecular weight compounds
  Crashing walnut with hammer!

## Slide 6: Introduction: Conceptual Reaction
Energy Input
Polymers
Gases
(CH4, C2H6)
Liquids
(Gasoline, Diesel)
Solids
(Carbon black,
Activated Carbon)
No oxygen
Reduction
Endothermic
400~700℃

## Slide 7: Design Target of Pyrolysis Reaction
Minimization of Energy Input
Maximization of Valuable by-products

## Slide 8
2. Pyrolysis Mechanisms

## Slide 9: Why pyrolysis mechanism is important?
Pyrolysis mechanism can elucidate PATHWAY to Valuable Products
Pyrolysis
Polymers
Desirable Products
Undesirable Products

## Slide 10: Why pyrolysis mechanism is important?

## Slide 11: Pyrolytic Degradation Pathways of Polyethylene

## Slide 12: Pyrolytic Degradation Pathways of Polyethylene

## Slide 13: Pyrolytic Degradation Pathways of Polypropylene

## Slide 14
3. Pyrolysis Kinetics

## Slide 15: Why pyrolysis kinetics is important?
Pyrolysis kinetics can elucidate 1) how fast the reaction is completed and 2) how the production rate of desirable products can be increased
Polymers
Desirable Products
Undesirable Products
kd
ku
Maximization of kd

## Slide 16: Pyrolysis Kinetic Models
MODEL I
MODEL II
Organic
Wastes
Gas
Liquid
Solid
K31
K41
K51
K11
Organic
Wastes
Gas
Liquid
Solid
K32
K42
K52
K22
Int
K21

## Slide 17: Pyrolysis Kinetic Models
MODEL III
Organic
Wastes
Gas
Liquid
Solid
K21
K52
K22
Int
K11
K31
K42

## Slide 18: Pyrolysis Kinetic Models
MODEL IV
Organic
Wastes
Gas
Liquid
Solid
K21
K42
K22
Int
K11
K51
K32

## Slide 19: Pyrolysis Kinetic Models
MODEL V
Organic
Wastes
Gas
Liquid
Solid
K21
K52
K22
Int
K11
K31
K42

## Slide 20: Pyrolysis Kinetic Model of Thermoplastics
Plastics
Gas
Liquid
Molten
State

## Slide 21: Pyrolysis Kinetic Equation
Kinetic Triplet
Arrhenius Parameters

## Slide 22: Pyrolysis Kinetic Equation
A Unique Thermal Reaction can be characterized by one set of Kinetic Triplet
Incorrect reaction model can mislead the Arrhenius Parameters as well

## Slide 23: Example: Polypropylene
What is the reaction model commonly
used for the pyrolysis of Polypropylene?

## Slide 24: Question
Is Reaction Order Function appropriate for representing the pyrolysis reaction model of Polypropylene?

## Slide 25: Evidences
Discrepancy of Activation Energy Values between Model-fitting and Model-free method
The reaction order function is usually applicable for homogeneous gas-phase kinetics, but the thermal degradation of polymers is accounted for by heterogeneous solid state mechanisms

## Slide 26: Activation Energy Values derived from model-fitting and model-free Methods
Methods |  | n | E (kJ․mol-1) | 
Model-fitting Methods | Freeman-Carroll |  |  | 
 | at 5 K/min |  |  | 
 |  | 1.57 | 338.15 | 
 | at 10 K/min |  |  | 
 |  | 1.69 | 346.63 | 
 | at 20 K/min | 1.38 | 290.13 | 
 | average | 1.55 | 324.97 | 
 | Catterjee-Conrad |  |  | 
 | at 5 K/min |  | 340.90 | 
 | at 10 K/min |  | 351.16 | 
 | at 20 K/min |  | 293.65 | 
 | average |  | 328.57 | 
 | Coats-Redfern |  |  | 
 | at 5 K/min |  | 316.71 | 
 | at 10 K/min |  | 315.62 | 
 | at 20 K/min |  | 321.02 | 
 | average |  | 317.78 | 
Model-free Methods | Friedman |  | 189.18 | 
 | Kissinger |  | 183.62 | 
 | Ozawa |  | 186.75 | 
Discrepancy of
E values

## Slide 27: How to identify Kinetic Triplet
How to Identify the Pyrolysis Reaction Model of PP and its Arrhenius Parameters
Kinetic Triplet

## Slide 28: How to identify Kinetic Triplet
Procedures Estimating Kinetic Triplet
Determining Reaction Model
Determining Reaction Constants
at various isothermal temperatures
Estimating Arrhenius Parameters
1st Stage
2nd Stage
3rd Stage

## Slide 29: How to derive g(a)
Derivation of
Kinetic equation
where
Integrating the kinetic equation

## Slide 30: Theoretical 13 models of RTPs
Reaction Models

## Slide 31: Procedures deriving Theoretical RTPs for 13 models
Procedures deriving Reduced Time Plots
Developing the following Relationship
Substituting serial numbers(0.1, 0.2 etc)
into  in the model equations and then
determining
Determining the reduced time from
4. Developing the reduced time vs. 

## Slide 32: How to determine pyrolysis reaction model of polymers
Fitting practices of experimental
RTP to theoretical RTPs
Best-fit of an experimental RTP
to a theoretical RTP

## Slide 33: Estimation of Arrhenius Parameters
Estimating the reaction constants at various isothermal conditions
Estimating A and E from Arrhenius Plot
Determination of Arrhenius Parameters

## Slide 34: How to obtain Isothermal Kinetic Data
Most previous studies have used commercial TGA that allowed
thermal decomposition that occurred during the course of
the temperature rise to the target temperatures
Time
Temp
Target Temperature
Undesirable decomposition happens
during the temperature rise
RTP requires decomposition pattern of polymers with time under isothermal conditions

## Slide 35: Thermobalance operated under pure static conditions
Weight Detection Part
Sample Loading Part
Pyrolysis Reactor

## Slide 36: Pyroltic Decomposition of PP under Dynamic Conditions(678~738K)`
Lower Temperatures
Higher Temperatures

## Slide 37: Reaction model of PP
Variation of Reaction Model with Reaction Temperature(R2A2)

## Slide 38: Estimation of Reaction Constant (k): PP
Lower Temperatures
Higher Temperatures

## Slide 39: Pyrolysis Reaction Model of PP
Lower Temperature Zones (650~700K)
  Contracting Cylinder Model
  E = 155 kJ/mol, lnA = 24.6 (A: min-1)
Higher Temperature Zones (>700K)
  Avrami-Erofeev Model
  E = 115 kJ/mol, lnA = 19.4 (A: min-1)

## Slide 40: Verification
Model-free methods
  Isothermal data
  Non-isothermal data
Model-fitting methods
  Differential
  Integral

## Slide 41: Model-free method using isothermal data
Compiling kinetic data at various isothermal operating temperatures
Developing a set of isoconversional data (=0.1, 0.2, 0.3, …)
Determining activation energy from the slope of the following equation:

## Slide 42: Model-free methods using non-isothermal data
Friedman method
Kissinger method
Ozawa method
Revised Ozawa method

## Slide 43: Activation energy(KJ/mol) values of PP
Model-fitting method
using Isothermal Data
(This study)
Model-free method
using Isothermal Data
Model-free method
using Non-isothermal Data
Model-fitting method
using Non-isothermal Data
Lower temperature regions
Higher temperature regions
103 71
112 83
118
Lower conversion regions
Higher conversion regions
140 112

## Slide 44: Activation energy(KJ/mol) values of PP

## Slide 45: Low Temeratures: Contracting-cylinder model
Heat is applied
Liquid State
Solid State
Evolution of volatiles at the surface
Isotropic shrinkage of melt

## Slide 46: Higher Temperatures: Avrami-Erofeev model
Liquid State
Bubble Nucleation is responsible for a major pyrolysis mechanism at higher temperatures
At the critical concentration of volatiles, bubbles may begin to nucleate
There may be a critical temperature where the highest molecular size of fragments is small enough to be vaporized, thus triggering the explosive generation of volatiles

## Slide 47: Implication
Rate of bubble nucleation appears to be limited by
the kinetics of heat, momentum or mass transfer
and thermodynamic properties of melt

## Slide 48
4. Pyrolysis Reactor Design

## Slide 49: Step for Effective Reactor Design
Investigating Pyrolysis Mechanism
  Determining REACTION PATHWAY
Estimating Pyrolysis Kinetic Model and Kinetics (Chemical Kinetics)
  Determining REACTION TIME
  Controlling REACTION PARAMTERS
Determining Scale-up Factors
Determining Temperature and Pressure Profiles of Reactor
Determining Reaction Rate and Time

## Slide 50
Thank You !