Materials Science and Engineering 445.302

“Phase Transformation”

Fall 2008

Professor Eun Soo Park

Syllabus

Course meeting times    Lectures: Two sessions / week

1.25 hour / session

Level: undergraduate

Text:       D.A. Porter and K.E. Eastering

“Phase Transformations in Metals and Alloys”

Chapman & Hall

References:  Paul G. Shewman, “Diffusion in Solid”, TMS (1989)

Reed-Hill, “Physical Metallurgy Principles”, PWS–Kent (1992)

Additional reading materials will be provided.

Course Description:

This course presents a unified treatment of the thermodynamics and kinetics of phase transformations from phenomenological and atomistic viewpoints. Phase transformations in condensed metal and nonmetal systems are discussed. This course begins with reviewing the principles of thermodynamics, phase equilibriums, diffusion, and crystal interfaces. The topics include absolute reaction rate theory, thermodynamics of irreversible processes, thermodynamics of surfaces and interfaces, chemical kinetics, nucleation and growth, spinodal decomposition, order-disorder transformations, diffusional transformations, martensitic transformations, coarsening, glass transition. At the end of the semester, you should understand the concepts, experimental technique, and open question in the transformation phenomena of various materials.

Chapter 1   Thermodynamics and Phase Diagrams

Chapter 2   Diffusion

Diffusion Mechanism

Diffusion Equation and Its Solutions

High Diffusivity Path

Diffusion in Multiphase Binary Systems

Chapter 3   Crystal Interfaces and Microstructure

Interfacial Free Energy

Boundaries in Single Phase Solids

Interphase Interfaces in Solids

Interface Migration

Chapter 4   Solidification

Nucleation in Pure Metals

Growth of a Pure Solids

Solidification of Single Phase Alloys

Eutectic Solidification

Chapter 5   Diffusional Transformations in Solids

Homogeneous Nucleation

Heterogeneous Nucleation

Precipitate Growth

TTT Diagrams

Precipitation in Age-Hardening Alloys

Spinodal Decomposition

The Precipitation of Ferrite from Austenite

Ordering Transformation

(Chapter 6)  Diffusionless Transformation

Characteristics of Diffusionless Transformation

Martensite Transformation

Components of Your Grade:

1) Exams (mid: 25% + final: 25%)

There will be two exams, each of which takes place in class for 1.5 hours. The exams will be conceptual and difficult.

2) Quizzes (10%)

There will be two short quizzes in between the major exams. These will take place in class and last for 30 minutes.

3) Homework (10%) and attendance (5%)

Problem sets are planned, to be handed out on Thursdays and due the following Thursday in class. The problem sets will likely be more mathematical than conceptual.

4) Reports and Presentation for Materials Design (25%)

Topics for phase transformation will be discussed or distributed, and every group will write a~3 page proposal, reports (mid term and final), and presentation (final).

Course Policies, Questions and Answers

Q: Will there be a recitation section?

A: None is planned, but if you really want one, speak up. We can negotiate.

Although most class periods will be lecture, I am hoping that the weekly class meetings will proceed in a discussion style format, so please do ask questions.

Q: What is the policy for attendance?

A: Please avoid a pattern of coming in late.

Q: What is the policy for late homework?

A: You lose 20 % of the full assignment value per day late. Since Psets are due on Thursday, you can get 80 % credit if you turn it in on Friday, 50 % on next Tuesday, nothing thereafter.