Phase Transformation: Quiz #2

Nov. 8, 2008

- (10%) Find a general solution for c(x,t) in non-steady state diffusion using the separation of variables.

- (10%) Derive Fick’s second law for substitutional alloys.

- (20%) Using Gibbs-Duhem equation, show that

Di= MRT

- (10%) Derive a relationship between  and  and use the result to derive JB for a A-B binary system with a strain energy gradient.

- (10%) Estimate the surface energy of {111}, {200}, and {220} surface planes in an fcc crystal. Express your answers in J/surface atom and J/㎡.

- (10%) Explain the Widmanstatten morphology shown in a transmission electron micrograph (see the figure below) of Al-4 at%Ag system as to (a) the needle-like shape and (b) angles between needles.

Fig. 3.42 p153 줄여서 붙일 것

(it continues to next page)

- (10%) The free energy difference between two grains is G. Estimate the velocity of grain boundary as a function of free energy term.

- (10%) Estimate the average grain size D which is in equilibrium in force with dragging solutes for a grain structure. The radius and volume fraction of the solutes are r and f, respectively.

- (10%) Describe briefly the effect of surface and strain energies on the shape of second phase in a matrix.

Answer the following question.

I missed (             ) classes during 10/5 –11/7/08.