Phase Transformation: Quiz #3

Dec. 12, 2008

- (15%) Two steel bars were joined and placed in a furnace for diffusion. The bar on the left side bar has C1 and one on the right has C2 wt. % of carbon and the diffusivity of carbon is D. Develop an equation for the carbon concentration of the bar on the right side as a function of time and distance.

- (15%) Using Gibbs-Duhem equation, show that

Di= MRT

- (15%) (a) Show that the angle term, S(), is equal to (2 + cos)(1 – cos)2/4 in the heterogeneous nucleation in a liquid melt and (b) calculate the critical volume, V*, of nucleus when the contact angle,  is 30o

- (15%) Derive, during dendritic growth in pure metal liquid, a relationship between the growth velocity of a dendrite and supercooling in front of the dendrite. Find the max. growth velocity of dendrites as a function of critical radius of the dendrite for nucleation.

- (30%) For steady state solidification of a binary A-B alloy, the following equation holds when the system experiences a limited liquid diffusion with no diffusion in solid.

XL=XO

XL and XO are the liquid and initial compositions while k, x, D, and v stand for the partition coefficient, distance from the solid-liquid interface, diffusivity of solute, and growth rate, respectively. (a) (5%) Explain the constitutional supercooling with a critical cooling rate at the solidification front of an alloy, (b) (15%) calculate the critical temperature gradient and (c) (10%) if the diffusion above is unlimited in liquid, find out the liquid composition when the weight fraction of liquid, fL, reaches 0.5 in the solidification. Note: the alloy contains 8 mole % of B in A and the partition coefficient is 0.5.

- (15%) (a) List the terms which determine the driving force for the nucleation in solid and (b) show that the critical radii of nuclei are the same for homogeneous and heterogeneous nucleation.

- (15%) Show the relationship, graphically and mathematically, between temperature and growth velocity for the diffusion-controlled growth of an incoherent precipitate,  of C   in  matrix of Co. Assume the precipitate is in the form of slab and the equilibrium composition at the interface is Ce. Hint: first, show the relationship between the velocity and compositions.

- (15%) (a) Derive the free energy change in spinodal decomposition when the compositional fluctuation starts by X from Xo and (b) show the nucleation-growth and coherency spinodal regions in the phase diagram. Draw the region boundaries based on the free energy diagram.

- (15%) (a) Explain the main cause of massive transformation in Cu-38 at.% Zn system and (b) list the kinds of order-disorder transformation and explain in terms of G, H and Cp.

Answer the following question.

I missed (        ) classes during 11/10/08 – 12/10/08

Have a Merry Christmas!