Midterm of Crystal Mechanics

2010. 11. 10.

- (30 points) Show that the compliances Sij of hexagonal symmetry material as follows, and derive the Young's modulus as function of S11, S33, S44, S13 and direction cosine a13.

- (20 points) Explain Zener’s anisotropic ratio in cubic material and the difference in elastic properties between Mo, Ag and W.

- (20 points) Explain the biaxial modulus in thin solid film with cubic crystalline structure under the equaibiaxial stress state.

- (10 points) Consider a FCC with a tensile stress parallel to <001>, <011> and <111> types of directions. How many initial slip systems operate for these respective cases ? (10 points) Determine the initial active slip system of the FCC under the tensile stress along the [112] axis of the crystal. (10 points) If CRSS is 50 MPa, what is the tensile yield stress at which the crystal will start to deform plastically?