Finial Exam of Crystal Mechanics

2010. 12. 8.

- (20 points) Can the {110}<001> family of slip systems in a cubic crystal produce any arbitrary strain without change in volume?

- (20 points) A plane strain compression test is carried out on a rectangular fcc single crystal, in which the compression direction is = [100] and the elongation direction is x1 = [011]. Which slip systems will operate and what will the compressive yield strength and Talyor factor be? You can use this equation and Table 1.

dw = A- B+ 2F+ 2G+ 2H

where A =-, B =-, C =-, F =, G =, H =

- (20 points) Explain the Sachs model, Taylor model, and self-consistant method including the CP-FEM in plastic deformation of polycrystalline materials.

- (20 points) Explain the deformation of martensite transformation.

- (20 points) Consider a carbon atom located at the interstitial site (0,0,1/2) within the body centered cubic structure cell. If the crystal undergoes deformation twinning with (112) as the composition plane and [-1-1 1] as the shear direction, in which kind of interstitial site is the carbon atom located after twinning ? You can use this equation.

= --+2

Table 1. Stress states for {111}<110> or {110}<111> slip.

| Number of stress state | A | B | C | F | G | H | Slip systems | Number ofof of active slip systems |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  | a1 | a2 | a3 | b1 | b2 | b3 | c1 | c2 | c3 | d1 | d2 | d3 | of active active slip |
|  | unit: (c | 111 | -1-1 1 | -1 1 1 | 1-1 1 | slip systems |
|  |  | 0101-1 | -1-101 | 1-1-10 | 0-0-1-1 | 10101 | -1-110 | 0101-1 | 10101 | -1-1-10 | 0-0-1-1 | -1-101 | 11110 |  |
| 1 2 3 4 5 6 7 8 9 10 11 12 13 14 15 16 17 18 19 20 21 22 23 24 25 26 27 28 | 1 0 -1 0 0 0 1/2 1/2 -1 -1 1/2 1/2 1/2 1/2 1/2 1/2 0 0 0 0 -1/2 -1/2 -1/2 -1/2 0 0 0 0 | -1 1 0 0 0 0 -1 -1 1/2 1/2 1/2 1/2 0 0 0 0 -1/2 -1/2 -1/2 -1/2 1/2 1/2 1/2 1/2 0 0 0 0 | 0 -1 1 0 0 0 1/2 1/2 1/2 1/2 -1 -1 -1/2 -1/2 -1/2 -1/2 1/2 1/2 1/2 1/2 0 0 0 0 0 0 0 0 | 0 0 0 1 0 0 0 0 1/2 -1/2 0 0 1/2 -1/2 1/2 -1/2 0 0 0 0 1/2 -1/2 1/2 -1/2 1/2 1/2 -1/2 1/2 | 0 0 0 0 1 0 1/2 -1/2 0 0 0 0 0 0 0 0 1/2 -1/2 1/2 -1/2 1/2 1/2 -1/2 -1/2 1/2 -1/2 1/2 1/2 | 0 0 0 0 0 1 0 0 0 0 1/2 -1/2 1/2 1/2 -1/2 -1/2 1/2 1/2 -1/2 -1/2 0 0 0 0 -1/2 1/2 1/2 1/2 | + - - + + - - + + + + - - - - + | - + + - - - + + - + - - + + + - | - + - + + + - - - - + + + - - + | + - + + + - - + + + + - - - + + | - + - - - - + + - + - - + + - - | - + + - + + - - - - + + - + + - | + - + - + - - + + + - + - - + - | - + + + - - + + + - - - + + + + | - + - - + + - - - - + + - + - - | + - - - + - - + + + - + - - - - | - + - + - - + + + - - - + + - + | - + + + + + - - - - + + + - + + | 8 8 8 8 8 8 8 8 8 8 8 8 6 6 6 6 6 6 6 6 6 6 6 6 6 6 6 6 |

, , , , ,