## Slide 1: Chapter 5 Ionic Chain Polymerization

## Slide 2: 5-1 Comparison of Radical and Ionic Polymerizations
Monomer
  Radical polymerization : almost all vinyl compound
  Ionic polymerization : very selective
    ex)Anionic : vinyl compound w/ e.w.g.
    Cationic : vinyl compound w/ e.d.g.
    See page 200 Table 3-1 (next page)
Radical & condensation polymerizations are well defined,
while ionic polymerizations are not. Why?
  Experimental difficulty
    : difficult to get reproducible data
    ∵propagating sites are carbocations or carbanions
    ⇒ very reactive extremely sensitive to impurity
  Reaction media is not clear
    : initiator, propagating molecule can be heterogeneous

## Slide 4
Characters of propagating chain end in cationic polymerization
  ⇒ polar covalent bond(Ⅰ), contact ion pair(Ⅱ),
  solvent-separated(or loose) ion pair(Ⅲ), free ion(Ⅳ)
    Ⅰ and Ⅱ → living carbocationic polymerization
    Ⅲ and Ⅳ → conventional uncontrolled carbocationic polymerization
Other classification
  Free ion : Ⅳ
  Ion pair : Ⅱ, Ⅲ
  Covalent species : Ⅰ ⇒ very slow or no reaction
Effect of solvent on the ion pair
  High polarity solvent → loose ion pair (Ⅲ)
  Low polarity solvent → tight ion pair (Ⅳ)
  ⇒ (+) & (-) charge separation is easier for high polarity solvent`
⇒
Major propagating species
Coexisting in equilibrium with each other

## Slide 5
Solvent effect on anionic & cationic polymerization
  Cationic : ⇒ [(BF3)OH]-, (AlCl4)-
  Larger counter ion : non reactive
  ∴ less affected by solvent polarity
  therefore even less polar solvent can make ion pair
  Anionic : ⇒ Li+, Na+
  Small counter ion
  ∴ much more solvent-dependent
Termination in ionic polymerization
  By the rxn of propagating chain with counter ion, solvent, or other species
  Not by the bimolecular reaction between two propagating polymer chains

## Slide 6: 5-2 CATIONIC POLYMERIZATION OF THE CARBON–CARBON DOUBLE BOND
  ∴ HCl cannot be used as an initiator.
  Possible initiators
    Perchloric, sulfuric, phosphoric, fluoro, chlorosulfonic, methanesulfonic, trifluoromethanesulfonic acids
    ⇒ Large counter ion, A- , just stabilize carbocation by solvation or complexation
    Still max. M.W. obtained is a few thousand
    ∵ A- is still reactive
5-2a Initiation
1. Protonic acid (Brønsted acid)
  A- should not be nucleophilic

## Slide 7
2. Lewis acid (+generally coinitiator)
  ⅰ) Lewis acid
    Metal halide : AlCl3, BF3, SbCl5, ZnCl2, TiCl4
    Organometallic derivatives : RAlCl2, R2AlCl, AlR3
    Oxy halide : POCl3, Cr2OCl
  ⅱ) Coinitiator
    Proton donor (protogen)
    → H2O, HX, alcohol, carboxylic acid
    Carbocation donor (cationogen)
    → t-butyl chloride, triphenylmethyl chloride
  Ex)
  ⇒ BF3OH- & AlCl4- : large & much less nucleophilic
  ∴ high M.W. can be obtained
    I : coinitiator
    ZY : initiator
    M : monomer
ⅲ) General initiation process by Lewis acid

## Slide 8
※ Self-ionization
  Without coinitiator, higher strength Lewis acid (AlCl3, TiCl4, etc.)
  ∴initiation is possible
    Ex)
  Increased initiation of Lewis acid mixture
    Ex)

## Slide 9
  Evidence of self-ionization
    → H2O conc. In the glove box : 10-3M
    ∴ H2O can act as coinitiator at any time
    Using sterically hindered pyridine (SHP)
    → Proton scavenger : react w/ H+
    Not Lewis acid or carbocation scavenger ∵steric hindrance
    - SHP + monomer + only Lewis acid
    1) Inhibition : SHP react w/ H+
    ⇒ initiation w/ H2O (coinitiator) in the glove box
    2) No inhibition
    ⇒ initiation by self-ionization
    initiation w/o H2O

## Slide 10
  General rule
    K & ki : both increase w/ increasing acidity of Lewis acid and coinitiator
    Ex) Lewis acid
    AlCl3 > AlRCl2 > AlR2Cl > AlR3 : the more Cl, the higher acidity
    AlR2I > AlR2Br > AlR2Cl : I > Br > Cl
    HCl > CH3COOH > PhOH > H2O > alcohol
    → protonic acid : coinitiator
  Exceptions
    Boron halide + H2O
    acidity: BBr3 > BCl3 > BF3
    activity (K & ki) : BF3 > BCl3 > BBr3
    ⇒ due to hydrolysis of BX3
    Hydrolysis reactivity
    BBr3 > BCl3 > BF3
Activity of an initiator/coinitiator complex
  ⇒ depend on the ability to donate a proton or carbocation to monomer

## Slide 11
Activity of cationogen
Primary & secondary halide are ineffective for initiation
  ∵ Carbocation is not easily formed
  ∴ Tertiary halide is used Ex)
⇒ is formed : having similar stability compared to
    or
    less stable than
  Ex)
    ⇒ more stable than the propagating chain end of styrene & isobutylene
    ∴ Cannot be used as coinitiator
    However they can be used for vinyl carbazole
⇒
Propagating radical

## Slide 12
ratio of initiator to coinitiator
→The polymerization rate increases with increasing [initiator]/[coinitiator], reaches a maximum, and then either decreases or levels off.
SnCl4-initiated polymerization rate of styrene in carbon tetrachloride at 25 oC. Symbols o (0.08 M) and  (0.12 M) initiator concentrations
The decrease in rate at higher initiator concentration is usually ascribed to inactivation of the coinitiator by initiator
such as SnCl4-H2O may involve
hydrolysis of Sn-Cl bonds to Sn-OH.

## Slide 13: 5-2b Propagation
⇒ Rearrangement in propagation (or isomerization) is possible due to 1,2-hydride & 1,2-methide shift
Because other carbocations are of comparable stability
polymerization of 3-methyl-1-butene

## Slide 14
Cationic polymerization of 4-methyl-1-pentene
Monomers w/o rearrangement,

## Slide 15
Other isomerization polymerization
  1. Intra-inter molecular polymerization
  → conjugated dienes
  Ex)
  2. Transannular polymerization
  Ex1)

## Slide 16
  Ex2) 5-methylene-2-norbornene
Polymerization by strain relief
Other polymers
Carbocation stability
Less sterically hindered

## Slide 17: 5-2c Chain Transfer and Termination
5-2c-1 β-Proton Transfer
1. Chain transfer to monomer ; + charge is transferred to monomer
  ⅰ) Transfer of a β-proton (proton transfer)
  ⅱ) Hydride ion transfer from monomer (hydride transfer form the H in sp3 C)
  ∴ For isobutylene ⅰ) is major C.T. to monomer rxn
β
β
β

## Slide 18
  ※ If the rxn temp. is higher than 20℃,
  the C.T. to monomer can be principle rxn that limits M.W.
  Below 20℃, C.T. to monomer is not significant.
  ∵ C.T. involves bond cleavage – need high activation E
2. Chain transfer to counter ion
: spontaneous termination
  ⇒ This termination should not be a dominant compared to C.T. to monomer
  ※ Polymer chemists are smart enough not to use such initiators
  ※
  ⇒ Only proton transfer is possible, while
  hydride transfer is not possible for these monomers

## Slide 19
5-2c-2 Combination with Counterion
→ when counter ion is nucleophilic : when protonic acid was used as an initiator
or
  ※ When Lewis acid was used
  Why?
  bond strength
  : B-F > B-O > B-Cl
  146 128 100 kcal/mol
B-O bond cleavage
B-Cl bond cleavage

## Slide 20
※ aluminum alkyl–alkyl halide initiating systems
- Termination by alkylation
- Termination by hydridation:

## Slide 21
5-2c-3 Chain Transfer to Polymer
ⅰ) Intra molecular electrophilic aromatic substitution
    ⇒ Back-biting
  ⅱ) Intermolecular hydride transfer to polymer
  → 1-alkene polymerization
    : 3o carbocation → branch generated!

## Slide 22
5-2c-4 Other Transfer and Termination Reactions
Chain transfer agents XA : present as solvent, impurity, or deliberately added to the reaction system
  Reinitiation is possible from
  ∴ Small amount of H2O : may not affect the polymerization rate
  Excess amount of H2O : inhibitor or retarder
  ∵ hydrolysis of initiators such as MX3
  To stop the cationic polymerization
  → Add excess amount of H2O, alcohol, etc.
- amines, triaryl or trialkylphosphines, and thiophene act as inhibitors or retarders by converting propagating chains to stable cations

## Slide 23: 5-2d Kinetics
  ⅰ) initiation
ex)
  ii) propagation
5-2d-1 Different Kinetic Situations

## Slide 24
  ⅲ) Termination
    → if by combination w/ counter ionEx
  Using steady state assumption
  ※ Radical polymerization
  ∴

## Slide 25
If there are chain transfer rxns,
  ⇒ Chain transfer decrease the while Rp is not affected (in general)
  since reinitiation w/ the proton derived from C.T. is fast
  ; the carbocation generated from C.T. is as reactive as M+ (propagating site)
  Exception
    : another termination
  Using steady state assumption (# of total active site is constant!)
: C.T. to solvent
: C.T. to monomer
: spontaneous termination or C.T. to counter ion
Stable, No reinitiation
∴ dead polymer
Decrease Rp

## Slide 26
Other case
  1) If R.D.S. of initiation is the first step
  2) Cationic polymerzation initiated by ionization radiation
  Initiation
  Termination by inhibitor
Radical ∙M- can also be generated
Termination by combination w/ counter ion
In Radical

## Slide 27
  3) Very pure system ; no impurity
  Then the only possible termination is
  ⇒ one cation is generated when one anion is generated
  If ionization radiation is used for initiation ⇒ Y-=e-
; combination by counter ion

## Slide 28
5-2d-2 Validity of steady state assumption
  1) Cationic polymerization is very fast
  Ex)
Ri > Rt
time
M+
S. S. assumption is valid only in very short period
  → In cationic polymerization, initiation is very fast!

## Slide 29
  2) Solubility?
  → initiating system & growing species can be insoluble in the rxn mixture
  ; salt are not soluble ①
  ∴ possibly heterogeneous polymerization
  ∵ solvents for cationic polymerization
  → Low polarity ; no rxn w/ carbocation ②
  ∙ Solubility also changed
  ∴ Rp expression in cationic polymerization is always erroneous
  To get more reliable Rp, [M+] should be determined
  How?
  ① Short-stopping of polymerization by an efficient terminating agent
  ② Stop-flow, rapid scan spectroscopy
insoluble
Partially insoluble
soluble
capillary
spectroscopy

## Slide 30
5-2e-2 Difficulty in interpreting rate constant
  → Most reported kp values are apparent or pseudo rate constant
  ⇒kpapp
Ion pair or free ion → both are possible w/ different rate constant
Free ion
Ion pair
Ion pair
Free ion
Some salt of carbocations can be crystallized ⇒ conc. can be obtained
% of Mf+ | 99 | 90 | 62 | 27 | 9 | 2 | 1 | 0.3
C/K | 10-2 | 10-1 | 1 | 10 | 102 | 103 | 104 | 105

## Slide 31
Most polymerization
Cationic polymerization is faster than radical polymerization
  ∴ Rp,cat ≫ Rp,rad
 | Kp [L/mol-sec] | kt | ki | [M+] or [M∙]
Cationic | 102 ~ 109 | 10-1 ~ 10-2 | 1 ~ 102 | 10-5
Radical | 102 ~ 104 | 106 ~ 108 | 10-2 ~ 10-4 | 10-7 ~ 10-9

## Slide 32
Reactivity of monomer
  → not enough data
  Vinyl ether > isobutylene > styrene, isoprene
Styrene derivatives
  p-OCH3 > p-CH3 > H > p-Cl > m-Cl > m-NO2
Probably due to the e- donating effect
e- donating

## Slide 33
CM and CS values
  Generally larger kp, lower CM
  Temp.↓ CM ↓ ∵ bond cleavage effect
  → not much data for the comparison

## Slide 34
  Solvent effect
  in general highly polar solvent, free ion is favored over ion pair
  ex)
  However, it is not always true
  ∵ Solvent polarity↑, kp+↓
 | Ε (dielectric constant)
CH2Cl2 | 9.72
CCl4 | 0.12
∵ free ion character decrease
Effect of reaction medium

## Slide 35
Pseudocationic polymerization
  Ex) Styrene + perchloric acid HClO4
  ⇒ propagation can proceeds through covalent species
  kpc : rate constant for propagating end w/ covalent bond, very small value
  solvent polarity↑, kpc constant or ↑

## Slide 36
High M.W.
Low M.W.
Elution time
Ph-NO2/CH2Cl2=1/7
Ph-NO2/CH2Cl2=1/15
CH2Cl2
CH2Cl2/benzene=10/1
CH2Cl2/benzene=2/1
Rxn solvent
Due to &
Due to kpc
G.P.C. results
  ⇒ Kc is faster than and
  then there would be unimodel molecular weight distribution
  Kc is obviously slower
  ∴ bimodal M.W.D

## Slide 37
7 criteria for living polymerization
by Quirk, poly. Int. (1992), vol.27
  1) Polymerization proceeds until [M]=0
  Addition of more monomer results in continuous polymerization
  2) Is a linear function of conversion
  ∴ not a sufficient criteria
  Number of polymer molecules remains constant
  → also possible when termination occurs w/o C.T.
  ∴ necessary but not sufficient
  4)
  if there is C.T. rxn, (obs) < (cal)
  Narrow molecular weight distribution
  ie.
conv.
Poisson M.W.D.
  ※ linear plot is also possible when termination occurs w/o C.T.
  Block copolymer preparation
  7) Quantitative chain end fuctionalization
  ⇒ found in many anionic polymerization, How about cationic polymerization?

## Slide 38
  ※ Requirement for Poisson M.W.D.
  ⅰ) growth occurs by consecutive addition
  ⅱ) all chain-ends are equally reactive
  ⅲ) all chain-ends, active-ends are present at start
  ⅳ) no chain termination or chain transfer
  ⇒ ki vs. kp ratio is very important
  ex) J. Chem. Phys. 28, 91 (1958)
  ∴ narrow M.W.D. is possible when kp / ki <10
  ※ Narrow M.W.D. is possible for other cases such as mixture
  ex)
kp/ki | P.D.I.
0.1 | 1.008
0.5 | 1.01
10 | 1.019
100 | ?
106 | 1.25
Living system

## Slide 39
Quasi-living carbocationic polymerization
  ⇒ Carbocations are so reactive that C.T. & terminations are facile
  ∴hard to get living system
  ⇒ 1980th Kennedy et al. at U. Akron
  ∙ Absence or reversibility of termination and/or C.T.
  ∙ Monomers are mostly consumed by propagation
  - See p.403 examples -
    Ex)
  ∙ The active-end is not a carbocation
  ∴ not very reactive
  ∙ The active-end is not totally covalent
  ∴ reactive
  ⇒ no termination, no C.T. ∴ pseudo living
+δ
+δ
-δ
-δ

## Slide 40
Energetics
  Using Arrhenius equation
  Ep for cationic polymerization ; positive but not much large < 20~25kJ/mol
  Et ; except the combination w/ counter ion
  all termination involves chain cleavage
  Ei ; case by case
  mostly involves the chain cleavage

## Slide 41
  If there is C.T.
→additional term
possible at higher temp.

## Slide 42: 5.3 Anionic Polymerization of the Carbon-Carbon Double Bond
Anionic Polymerization → similar to cationic polymerization
Difference from cationic polymerization
  1) Rate constant difference between is very large and
  in cationic
  2) is always positive
  ∴ Temp↑ Rp↑
  in cationic or
  3) Solvent for anionic polymerization
  → Aliphatic hydrocarbon, aromatic hydrocarbon, ether.
  → Due to the strong nucleophilicity of carbanion, halogenated solvent, ketone, esters can not be used.
  ※ in cationic polymerization, halogenated solvent can be used (except 3o carbon)
  4) Termination by transfer of a positive fragment such as H+
not very different

## Slide 43
Reactions of carbonion with
  1) Air
  2) Acid
  where H-A; ROH, RCOOH, RSH, RCH2(CO)R, PhCH3, C2H2, CH2=C=CH2
  → depend on the pKa of ( )
  3) Carbonyl group
  4) Halogenated compounds

## Slide 44
Monomer requirements for anionic polymerization
    ⇒ ∙ carbanion should be stabilized
    ∙ no side reaction
  1) Y = e--withdrawing or e--delocalizing substituent
  = -CH=CH2, -Ph, -CO2R, -CN, -SO3R, -COR, -NO2
  Absence of acidic proton
  -COOH, -OH, -NH2, -C≡CN can not be used
  Absence of electrophilic substituent which react with anionic chain end
  -CN, -SO-, -SO2-, -C(O)R, -COOR, -NO2
  ∴ Possible monomers ( Table 3.1 p 200)

## Slide 47
Initiators
  ※ To initiate, the initiator should be more basic than the propagating chain end.

## Slide 48
5-3a-1 Nucleophilic initiator (basic initiator)
  → NaNH2, LiN(C2H5)2, alkoxide, hydroxide, cyanide, organometallic compounds (BuLi)
5-3a Initiation

## Slide 49
5-3a-2 Electron transfer initiator
<1% radical polymerization
>99% anionic polymerization
  i) Naphthalene anion-radical transfer
Very fast

## Slide 50
  ⅱ) Lithium in liquid ammonia
  ⅲ) Ionizing radiation
∙∙
↓dimerization
↓polymerization
stable

## Slide 51
5-3b Termination
5-3b-1 Polymerizations without Termination
⇒ possible for a certain degree because termination by combination
of the anion with a metal counterion does not take place.
Ex) anionic polymerizations of nonpolar monomers such as styrene and 1,3-butadiene
5-3b-2 Termination by Impurities and Deliberately Added Transfer Agents

## Slide 52
  ∵ hydride elimination is possible even in most stable styrene
5-3b-3 Spontaneous Termination
hydride elimination
The order of stability of polystyryl carbanions : K > Na > Li.
Stability according to polarity of solvent
  Polystyrly carbanion : less stable at higher temp. in polar solvent THF, DME.

## Slide 53
5-3b-4 Termination and Side Reactions of Polar Monomers; :
such as acrylates

## Slide 54
Desirable anionic polymerization of acryl monomer
Other side reactions

## Slide 55
5-3d Kinetics of Living Polymerization
5-3d-1 Polymerization Rate
In cationic
Free ion
Ion pair
In Radical
Anionic kpapp values :
10–100-fold lower than in radical polymerization in hydrocarbon solvents,
10–100-fold higher for polymerizations in ether solvents.
[M∙] = 10-9 – 10-7 M
[M-] = 10-4 – 10-2 M
Thus anionic polymerization rates are much higher than radical rates
based only on the concentrations of propagating species.
where [M-] is the total concentration of all types of living anionic propagating centers (free ions and ion pairs).

## Slide 56
In cationic
In Radical

## Slide 57
5-3d-2 Effects of Reaction Media
  ⇒ The increase in kpapp with increased solvating power
  ∵ the increased fraction of free ion
  ⇒ DME > THF
  ∵ DME have two ether bond in a same molecule
  → increased solvating power

## Slide 58
5-3d-2-a Evaluation of Individual Propagation Rate Constants for Free Ions and Ion Pairs.
where P- is free propagating anion and P-(C+) is the ion pair
because
where [M-] is the total concentration of all types of living anionic propagating centers (free ions and ion pairs).

## Slide 59
The extent of dissociation is small under most conditions, then [M-]  [P-(C+)]
[M-] = [P-] + [P-(C+)]
because
because
The two propagating species are in equilibrium
If there is no source of either ion other than P-(C+)

## Slide 60
If polymerizations in the presence of excess counterion by adding a
strongly dissociating salt (e.g., NaB4 to supply excess Na+).
Then the concentration of free ions, depressed by the common ion effect, is given by
because
[M-]  [P-(C+)]
When the added salt is strongly dissociated and the ion pairs slightly dissociated, the counterion concentration is very close to that of the added salt [CZ]:

## Slide 61
Polymerization of styrene by sodium naphthalene in 3-methyltetrahydrofuran at 20 0C
can be obtained

## Slide 62
Polymerization of styrene by sodium naphthalene in 3-methyltetrahydrofuran at 20 0C in the presence of sodium tetraphenylborate.
can be obtained

## Slide 63
5-3d-2-b Reactivity in Anionic Polymerization.
[M-]  [P-(C+)]
↑
K ↑
(Li > Cs)
Ion pair : solvent-separated + contact ion pairs
The fraction of solvent-separated ion pairs increases with increasing solvation
of the counterion.
Solvent-separated ion pairs are much more reactive than contact ion pairs (Sec. 5-3d-4).
In THF

## Slide 64
However, the effect of increasing counterion size levels off after k is approximately the same for potassium, rubidium, and cesium.
↑
(Li < Cs)
bond strength (carbanion center and counterion)  , from Li to Cs
In Dioxane

## Slide 65
5-3d-3 Degree of Polymerization
propagating species formed from sodium naphthalenes
(e.g., alkyllithium)

## Slide 66
anionic polymerization of styrene
  ; especially with regard to the multiplicity of propagating species
  Ionic species aggregate
  CIP : contact ion polar
  SSIP : solvent seperated ion pair
  In non polar solvent, the propagating center
  In polar solvent, the propagating center
: H.C.
Benzene
toluene
5-3d-4 Energetics: Solvent-Separated and Contact Ion Pairs

## Slide 67
Styrene propagation in H.C. solvent (nonpolar)
  See next page table 7.1
  Why?
  ⇒ aggregation
-Counter ion dependence of kp,obs
  ∵ kd increases increasing cation size
⇒ total chain end concentration
=

## Slide 69
Diene polymerization in non polar(H.C.) solvent
  ⇒ See table 7.1 for Isoprene & Butadiene case
  kinetic order 0.17~0.5 case by case

## Slide 70
Styrene propagation in polar solvent (THF, dioxane, DME, etc.)
  Presence of free ion is deduced by conductance & common ion effect
  Evidence for CIP, SSIP comes from JACS, 88, 307 (1996)
  ⇒ UV-Vis spectrum changed with temp., solvent, and M+
  not affected by common ion or dilution
  interpreted in terms of
  ◈ For M=Na
  exothermic
  ΔHo=-7.6 kcal/mol ΔSo<0
  ∴ T↑, K↓ [SSIP]↓

## Slide 71
  ◈ % SSIP↑ in the order Bu4N~C < Na < Li follows order of Lewis acidity
  i.e. Li+ is a strong acid and is strongly solvated
  % SSIP↑ as solvent strength increases
  DME ≥ THF > dioxane
  ex)∙J.A.C.S., 103, 5657, 1983
  studied 13C-NMR of Ph2-CHM+ in THF
  SSIP for Li
  Mixture of CIP/SSIP for Na
  CIP for K, Cs, Rb
  ∙J.P.S., 69, 612 (1965)
  for low free ion conc. α≪1
Accept the unpaired e-
↑ ↑
SSIP+SIP free ion

## Slide 72
  ◈

## Slide 73
  : Li > Na > K > Rb > Cs
  k – is independent of M+, ∵ free ion
  slope change reflects kd1/2 ( or K1/2 in the text ) , Li is most strongly solvated, kd is highest
  ⇒ highest % free ions for Li
  Dioxane : less polar solvent
  ∴ reactivity is proportional to the bond strength
  ⇒ same as non polar solvent
  Cs > K > Na > Li

## Slide 74
  ⇒ The increase in kpapp with increased solvating power
  ∵ the increased fraction of free ion
  DME > THF
  ∵ DME have two ether bond in a same molecule
  → increased solvating power
If NaBPh4 is added to PSNa
  kpapp changes from 2100 to 140 L mol-1 s-1
  ∵ common ion effect
  reduce the conc. of free ion!

## Slide 75
Temperature dependence of k -
  ln k - vs. 1/T is linear
  k – is independent of solvent
  ⇒ Eur. Polym. J., 11, 119 (1975)

## Slide 76
  However,
  k± shows a nonlinear dependence on T
  k± depends on solvent
Explanation
⇒Conc. Of SSIP
⇒Conc. Of CIP

## Slide 77
⇒ p.431 odian
THF
3Me-THF
CIP
SSIP

## Slide 78
In summary
PS M exist as multiple species in polar solvent ;
each contributes to propagation
  The relative populations depend on T, M+, solvent
  ⇒ k - = 10(kS) = 1000(kC)
  If the equilibriums are faster than,
  kC, kS, k -, then
Combination of kC&kS

## Slide 79
5-3d-5 Association Phenomena in Alkyllithium
For styrene polymerization by n-butyllithium in aromatic solvents, the initiation and propagation rates are proportionalto only the 1/6- and 1/2-powers of n-butyllithium concentration, respectively.
The macrocyclic crown ethers such as 18 crown-6 (XXIXa) and cryptands such as 2.2.2- cryptand (XXIXb) are extremely powerful for breaking up association of organolithium compounds.
to greatly increase the concentration of free-ion propagating species, resulting
in very large rate increases

## Slide 80
Crown Ether effect of MMA anionic polymerization
  DB-18-CE-6
  ∵ Chelation increases the effective size of the counter ion
Temp. (oC) | C.E./I | Mn | Mw/Mn
25 | 1 | 10500 | 1.40
25 | 2 | 10500 | 1.03
0 | 1 | 8500 | 1.20
0 | 2 | 8500 | 1.05
→ large effective
counter ion
radius

## Slide 81
Kinetics of polymerization with termination
  ⇒ Ri : the rate of initiation
  Propagation
  Chain transfer to solvent
  Chain transfer to adventitious water , also termination
  If there is steady state,
↘Conc. Of anionic propagating chain center

## Slide 82
5-4 BLOCK AND OTHER POLYMER ARCHITECTURES
5-4a Sequential Monomer Addition
  Block copolymer
  ex) Synthesis of PS-PMMA block copolymer
  ∴
  ∴ Sequence is very important
  ※ For Styrene-Isoprene, Styrene-butadiene Sequence is not important

## Slide 83
Crossover from one carbanion to another occurs only when the new carbanion is comparable or higher in stability than the original carbanion.
Poly(methyl methacrylate) carbanion is more stable than polystryrene carbanion. Carbanion stability can be estimated from the pKa of the conjugate acids of model carbanions.
Toluene and ethyl acetate have pKa values of 43 and 30, in line with the higher stability of the PMMA carbanion.
5-4b Telechelic (End-Functionalized) Polymers
  Containing one or more end functional groups

## Slide 84
  ⟹ Monofunctional telechelic polymers containing OH, NH2, COOH groups
  They can be used to obtain diblock copolymers.
amine-terminated telechelic polymers
styrene–isobutylene–styrene triblock polymer.

diethylaluminum chloride styrene

## Slide 85
5-4c Coupling Reactions
Living anionic polymers and block copolymers can be linked by coupling reactions.
the synthesis of star (multiarmed) polymers
CH3SiCl3, (ClCH2)4, and 1,2,4,5-tetrachloromethylbenzene also can be used
3-arm star with one polyisoprenyl (PI) and two polystyryl (PS) branches

## Slide 86
Using 1,3,5-tris(1-phenylethenyl)benzene to make tristar and Miktostar polymers

## Slide 87
5-4d Transformation Reactions
The anionic to cationic transformation
The anionic-to-radical transformation
⇒ Limitation:
A∙B both can propagate Anionic/cationic or anionic/radical polymerization

## Slide 88
  ⇒ Tc is very low except formaldehyde
  ⇒ ∵
  ΔS is approximately the same
5-6 CARBONYL POLYMERIZATION

## Slide 89
  ⅰ) Formaldehyde initiator
  → R- M+, RO- M+, RCOO-M+, amine, pyridine
  Initiation
  Propagation
  Termination
  ⅱ) Other carbonyl monomer other than HCHO
  ⇒ Stronger bases such as alkali metal alkyls & alkoxide are the initiator
  ◈
  1) Inductive effect : destabilize the propagating anion
  2) Steric effect
  ◈ X=F,Cl
  ⇒ stabilize the propagating anion
  ∴ Tc is higher than RCHO (Table 5.3)

## Slide 90
Cationic polymerization
  initiator : protonic acid (HCl, CH3CO2H), Lewis acid
  Initiation
  Propagation
  Termination

## Slide 91
  ⇒ competing side reactions
  ⅰ) cyclotrimerization (6-membered ring)
  ⅱ) Acetal formation
  ⇒ both can be minimized by polymerization at low temperature

## Slide 92
Hydrogen-Transfer polymerization
  Initiator : sodium, organolithium, alkoxide
  →strong base
  ⇒ yield is not very high
  ∵ possible side rxns

## Slide 93
Radical polymerization of carbonyl monomer
  ⇒ Generally not possible
  ⅰ) : polar compound
  ∴ not prone to attack by a radical
  ⅱ) most radicals are produced at temperatures above Tc of carbonyl monomer
  Several cases for radical poly. Of carbonyl monomers
  ⅰ) : Trifluoroacetaldehyde w/
  at 22℃
  ⅱ) using trialkylboron-oxygen redox initiator
  at -78℃
  ∴less polar system!
+δ
-δ
Less e- negative

## Slide 94
End-capping
  Polyacetals from carbonyl monomers are unstable at ambient temperature
  ∵ low Tc ⇒ practical application is limited
  ※ end-capping or end-blocking
  ex)
  ⇒ Reactive site (anion or cation) does not from at the chain end,
  then no depolymerization at Tc
  Polyoxymethylene (POM, Delrinⓡ) is commercial polymer
  150 million pound / year
  : highly crystalline 60~77%
  Tm=175℃ (ease of packing ∵flexible)
  higher than PEO(~60℃), PE(~140℃)
  ∵ higher polarity

## Slide 95
Monomers w/ two different polymerizable groups
  ∵
  both parts are sterically hindered
  ⇒ radical : homopolymer
  anionic : copolymer
Hydrogen transfer polymerization
radical, cationic, or anionic ?
No reactivity
Na
RLi
Vinyl group anionic polymerization is impossible
-NH2 acidic

## Slide 96
  How?
  ∴ ⅰ) hydrogen transfer
  ⅱ) active site is monomer anion
  ∴ While some units are generated
  depending on solvent, temp., concentration, initiator
There is some chances
→initiation
propagation
↑
Activatied monomer

## Slide 97
Polyisocyanate
  Nylon1
  liquid crystalline polymer ∵rigid backbone
  → anionically polymerized using
  low Tc
  ∴ predominant rxn at RT
Radical, cationic, anionic
  1) Ionic poly. : at low temp. w/ low activation energy
  Radical poly. : 50℃<
  2) Ionic poly. : sensitive to solvent, counter ion, solvent polarity
  ∵solvation ability
  Radical poly. : insensitive
  ∵ radical inself is organic
  no solubility problem
n R-N=C=O
Polymerization through N=C bonds
Through anionic polymerization